**Enhancement of dielectric properties and conduction mechanism in BaTi0.85Sn0.15­O3 for energy storage application**

Sagar Dutta1, Md. Shahjahan Ali2, Angkita Mistry Tama3, Md. Masud Parvez4,

Humayra Ferdous3,5, M.A. Hakim6, Md. Sarowar Hossain3,5\*

1Institute of Natural Sciences, United International University, Dhaka-1212, Bangladesh

2Department of Sciences, BGMEA University of Fashion and Technology, Dhaka-1230, Bangladesh

3Department of Physics, Faculty of Science and Technology (FST), American International University-Bangladesh (AIUB), Dhaka-1229, Bangladesh

4Bangabandhu Sheikh Mujibur Rahman Aviation and Aerospace University, Dhaka-1215, Bangladesh

5Center for Biomedical Research (CBR), Dr. Anwarul Abedin Institute of Innovation (DA2I2), American International University-Bangladesh (AIUB), Dhaka-1229, Bangladesh

6Department of Nanomaterial and Ceramic Engineering (NCE), Bangladesh University of Engineering & Technology, Dhaka-1000, Bangladesh

\*Corresponding author: [sakil\_phy@aiub.edu](mailto:sakil_phy@aiub.edu), sakil\_phy@yahoo.com

**Abstract**

To achieve cost effective materials with improved dielectric properties, BaTiO3 and BaTi0.85Sn0.15O3 have been prepared by solid state reaction technique introducing a two step sintering method. The structure of the samples has been investigated by X-Ray diffraction (XRD) and Raman spectra at room temperature (RT~300 K). In addition, crystallographic microstructures and grain morphology have been evaluated by transmission electron microscopy (TEM) and scanning electron microscopy (SEM) respectively. Apart this, the band structure along with density of states (DOS) are evaluated using first principle calculations for BaTiO3 and BaTi0.85Sn0.15O3. The band structure depicts bandgap of 1.80 eV and 1.82 eV for BaTiO3 and BaTi0.85Sn0.15O3 respectively. The DOS calculation displays the increase in hybridization of Ba2+ (A site) and Ti4+ (B site) cations with oxygen octahedra resulting in off-center displacement of cations in Sn doped BaTiO3 sample. A disordered cubic phase is obtained in BaTi0.85Sn0.15O3 sample sintered at 1350 ℃ resulting in the highest dielectric constant with a minimum loss . The conduction mechanism has been analyzed from the temperature and frequency dependence of resistivity . The overall forecasts indicate BaTi0.85Sn0.15O3 annealed at 1350 ℃ to be a potential candidate for energy storage capacitive devices in the electronic industry.

**Keywords:** Microstructure, Density of states, Orbital Hybridization, Off-center displacement, and Dielectric constant.