| Title: | The significance of bilayer window (CdS:O/CdS) on the performance of CdTe thin film solar cells |  |  |
| --- | --- | --- | --- |
| Author(s) Name: | N.K. Das, S.F.U. Farhad, A.K. Sen Gupta, E.M.K. Ikball Ahamed, M.A. Matin, N. Amin |  |  |
| Contact Email(s): | nowshad@aiub.edu |  |  |
| Published Journal Name: | Optical Materials |  |  |
| Type of Publication: | Journal |  |  |
| Volume: | 155 | Issue |  |
| Publisher: | Elsevier |  |  |
| Publication Date: | Sept. 2024 |  |  |
| ISSN: | 0925-3467 |  |  |
| DOI: | https://doi.org/10.1016/j.optmat.2024.115816 |  |  |
| URL: | https://www.sciencedirect.com/science/article/abs/pii/S0925346724009996?via%3Dihub |  |  |
| Other Related Info.: |  |  |  |

| Abstract: |  |
| --- | --- |
| Ultrathin and compact CdS:O/CdS bilayer window in CdTe solar cells has higher potential for enhanced p-type doping, reduced Te diffusion, and improved power conversion efficiency (PCE) compared to traditional single-layer CdS or CdS:O windows. In this effort, we used a two-gun RF sputtering equipment to deposit compact CdS:O (∼50 nm)/CdS(∼50 nm) bilayers onto the borosilicate and ITO-coated glass substrates at low temperature (≤250 °C). Intriguingly CdS:O/CdS bilayers retain its hexagonal {0002} preferential orientation but with around 10.58 % optical bandgap (Eg) increment compared to CdS (Eg ≈ 2.32 eV) of equal thickness (∼100 nm). Close-spaced sublimation (CSS) technique was used to deposit the CdTe thin film onto the CdS and CdS:O/CdS layers at 650 °C. The effect of CdS and CdS:O/CdS layers on the microstructural and morphological features of CdCl2-treated CdTe films were critically analyzed in revealing a promising {0001}/{111}-like partial-epitaxy presumably due to the preferential cubic CdTe growth along the <111> orientation. The CdTe films grown over a CdS:O/CdS layer exhibited smaller average crystallite and grain sizes than those grown over a single CdS layer. An essential finding was the formation of an optimal intermix layer of CdSxTe1-x, particularly evident in the CdTe films grown on the CdS:O/CdS bilayer. To comprehensively explore the effect of CdS:O/CdS window layers on PCE, complete CdTe solar cells were fabricated using three different window layers: CdS, CdS:O, and CdS:O/CdS, which are all considered as rudimentary as no layer optimization was performed. Notably, CdTe solar cell that incorporates the CdS:O/CdS bilayer window exhibited the most promising performance among all the tested rudimentary cells and corroborated the numerically simulated findings conducted by the SCAPS-1D simulator. |  |